	Canadian Natural Resources Limited

GENERAL PRESSURE VESSEL INFORMATION

	District: Grande Prairie Ab.
	Skid No.

	Facility: Elmworth Gas Gathering
	Location (LSD):  10 – 36 – 68 – 09 – W6M 

	Vessel Name & Equipment Number:  3 Phase Vertical Separator

	Orientation: Vertical

	Status:         Operating
	 Regulatory  Inspection 

	PRESSURE VESSEL NAMEPLATE DATA

	Registration Number

A 2651642
	CRN Number


K 1730.2

	Vessel serial number: P 1137A   
	Size: 20 in. OD x 8 ft.  S/S

	Shell thickness:  18.5 mm
	Shell material:  SA 516 70 N

	Head thickness:  18.0 mm
	Head material:  SA 516 70 N

	Tube wall thickness:
	Tube material:

	Tube diameter:
	Tube length:

	Channel thickness:
	Channel material:  

	Design pressure
	Shell:  1150 PSI
	Operating pressure
	Shell:

	
	Tubes:
	
	Tubes:

	Design Temp.
	Shell:  200 deg F
	Operating temperature
	Shell:

	
	Tubes: 
	
	Tubes:

	X-ray:  RT 1
	Heat treatment: Nil

	Code parameters: ASME VIII / Div 1
	Coated: No

	Manufacturer: Cessco
	Year built: 1990

	Corrosion allowance: 
	Manway:   6 inch Hand Hole

	PRESSURE SAFETY VALVE  NAMEPLATE DATA

	PSV Tag no.
	Manufacture
	Model
	Serial number
	Set Pressure
	Capacity
	Size

	431

430
	Farris

Farris
	2741U

2741U
	CE 1263 KD

CE 1265 KD
	1150 Psi

1150 Psi
	2213 Scfm

2213 Scfm
	.75 x 1

.75 x 1

	Serv By
	Date
	Block Valve
	CRN number
	Code Stamp
	Location
	

	Unified Valve
	Dec 04
	No
	Not Stated
	UV
	Inlet and outlet piping
	

	SERVICE CONDTIONS-INDICATE ALL THAT APPLY

	  Sweet  X
	Sour  
	 Oil
	Gas  X
	 Water  X

	 Amine
	LPG
	Condensate 
	Air
	Glycol 

	Other (Describe):


Inspection Interval ________________________________________PSV Service Interval_________________________________

(Determined by MIC in conjunction with Chief Inspector following guidelines of  CNRL’s Owner-User Inspection Program)
Reports reviewed and accepted by:
Mechanical Integrity Coordinator________________________________________________Date__________________________

Fill out all forms as completely as possible. All information is important!  Use back of sheets to record additional information or sketch if required.

Copy of report to be filed by MIC at site,  and copy sent to Chief Inspector

A # 2651642

	External Inspection Items


	G
	F
	P
	N/A
	                    Comments



	Insulation: Verify sealed around manways, nozzles, no damage present, and there is no egress of moisture.
	
	
	
	X
	Vessel is not insulated.

	External Condition:  Assess paint condition, areas peeling, record any corrosion, damage, etc (record location, size and depth of corrosion or damage)
	
	X
	
	
	No loose or flaking paint.

	Leakage: Record any leakage at flanges, threaded joints, weep holes on repads, etc.
	X
	
	
	
	No leaks detected.

	Skirt:       Assess condition of paint, fire protection, concrete. Look for corrosion, buckling, dents, etc. Look at vessel surface area near supports. Verify no signs of leakage at attachment to vessel and attachment welds are acceptable. Ground wire attached?
	X
	
	
	
	Separator is mounted firmly to skid deck.

Skid Package is grounded.

	Anchor Bolts:    Hammer tap to ensure secure. Look for cracking in treads or signs of deformation.
	X
	
	
	
	Firmly bolted.

	Concrete foundation: Check for cracks, spalling, etc. 
	
	
	
	X
	

	Ladder / Platform:    Describe general condition,  ensure support is secure to vessel, describe any hazards. 
	
	
	
	X
	

	Nozzle: Assess paint, look for leakage, and ensure stud threads are fully engaged. Record any damage, deflection, etc. Are nozzles gusseted?
	X
	
	
	
	Good condition, no leaking detected.

	Gauges: Ensure gauges are visible, working, no leakage, and suitable for range of MAWP/ Temp.
	X
	
	
	
	Firmly attached and within operational parameters for service.

	External Piping:  Ensure pipe is well supported. All clamps, supports, shoes, etc. in place. Look for evidence of structural overload, deflection, etc. Paint condition, external corrosion?
	X
	
	
	
	Firmly supported, no distortion or deflection.

	Valving:  Ensure no leaks are visible. Valves are properly supported and chained if necessary.
	X
	
	
	
	Firmly attached, no leaks.

	PSV: Ensure PSV is set at pressure at or below that of vessel. 
	
	
	
	
	Located on Inlet and Discharge Piping, set at MAWP of vessel.

	NDE methods: Was UT/ MPI done on vessel
(MI coordinator to review results)
	X
	
	
	
	Ultrasonic thickness survey carried out – No items of concern.

	Recommendations or corrective actions :  Vessel is Fit for  Service or describe corrective actions required)
(MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented)

1. No recommendations at this time – return vessel to service. 

Summary: This vessel is in good condition, ultrasonic corrosion survey carried out – no metal thickness detected below nominal minus corrosion allowance.

Vessel is fit for service.




Inspected By:  D. Wiedman                                                                                                                                          Date: Dec 2004

3 Phase Vertical Separator – A 2651642

	Internal Inspection Items


	G
	F
	P
	N/A
	                    Comments



	Coating:

Assess coating. Describe area coated, general condition of coating. 
	
	
	
	X
	

	Hand Hole access:
	X
	
	
	
	Good condition, no pitting to nozzle or to flange face.



	Bottom head:
	X


	
	
	
	Good condition – cleaned out – no pitting.

	Top head:
	
	
	
	X


	No access.

	Shell:

 Record location, size and depth of all erosion, corrosion or mechanical damage. Describe 

General condition.  
	X
	
	
	
	Limited viewing to lower shell. Good condition, no pitting. 

	Welds:
	X
	
	
	
	Good condition, no corrosion to welds.



	Flange Face:  

Record location, size and depth of all erosion, corrosion or mechanical damage. Describe 

General condition.
	X
	
	
	
	Good condition, no corrosion or pitting to gasket seating face.

	Anodes:
	
	
	
	X
	

	Divider:
	X
	
	
	
	Good Condition, intact and in place.



	Demister:
	X
	
	
	
	No access to demister.



	Float:
	X
	
	
	
	Good, intact and in place. 



	Internal piping:
	X
	
	
	
	Good condition, intact and attached.

	NDE Inspections
	X
	
	
	
	No NDE inspections at this time.

	Recommendations or corrective actions (indicate if fit for service) 

1. Return vessel to service.

Summary: This vessel is in good overall condition, no pitting detected.


Inspected By: Dellas Wiedman

Date: December 18 – 2004 

3 Phase Vertical Separator – A 2651642

[image: image1.jpg]Y-

MiN. DESIOGN M

AL TEMP.

SERIAL NG, YEAR BUILY

REG, DESIGN N@. VOLUME

4 2 i i : -

L THICKNESS SHELL MAT . WEIGHT

INSPECTOR



[image: image2.jpg]



[image: image3.jpg]


[image: image4.jpg]



3 Phase Vertical Separator – A 2651642

Float and deflector – intact and attached – Shell has no pitting. Bottom head has general scaling and surface corrosion – no pitting

[image: image5.jpg]


[image: image6.jpg]



[image: image7.jpg]


[image: image8.jpg]



Bottom head – circ weld and drain nozzle – no obstruction to nozzle and no corrosion to weld.

�





�





�





�





�





�





�





�








